Molecular Formula: CeH2~3

Purity: 99.5%

Specification:- 100 mesh / - 200 mesh

CAS:13864-02-3

EINECS No.:237-608-2

# Cerium hydride(CeH2~3)-Powder

Characteristic

Cerium metal (γ-phase) at room temperature possesses the face-centered cubic (fcc) structure. Upon incorporation of hydrogen and beyond its solubility limit, CeH2 is first formed as the hydride H− ions occupy the tetrahedral sites in the fluorite fcc structure. Increasing hydrogen stoichiometry leads to a series of well-defined H-stoichiometry and temperature dependent structures. As the additional H− ions occupy the octahedral sites, the highest stoichiometry of CeH3 is achieved, possessing a BiF3-type structure.

Appearance：Powder

Molecular weight：143.14 g/mol

Density (near r.t.)：5.5 g/cm3

Chemical Composition

| Rare Earth Impurity(≤) |  |  | Ce/RE |  | ≥99.5% |  |
| --- | --- | --- | --- | --- | --- | --- |
| Item | La/RE | Pr/RE | Nd/RE | Sm/RE | Y/RE |  |
| Content(%) | 0.052 | 0.074 | 0.017 | 0.010 | 0.010 |  |
| Non-Rare Earth Impurity(≤) |  |  | RE |  | ≥99% |  |
| Item | Fe | Si | Ca | Mg | Al | C |
| Content(%) | 0.087 | 0.026 | 0.012 | 0.018 | 0.013 | 0.027 |

Granularity of materials- 200 mesh

Application

- Among many metal hydrides, rare earth metal hydrides represented by cerium hydride are favored by researchers in the field of energetic materials due to their high chemical potential and reactivity.

- Cerium hydride is also widely used as a hydrogen storage material.

Package:

Vacuum pumping and argon protection, 500g or 1000g / bottle