Molecular Formula: YbB6

Purity: 99.9%

Specification:- 360 mesh / - 500 mesh

CAS:12008-33-2

EINECS No.:234-540-5

# Ytterbium Boride (YbB6)-Powder

Characteristic

Ytterbium Boride Powder, also called Ytterbium Hexaboride, is one of the rare earth borides, the molecular formula is YbB6. Ytterbium hexaboride is black crystalline powder. Among all REB6, YbB6 is especially attractive for its relatively low density, high mechanical strength, and high melting point characteristics. The crystalline form of YbB6 has cubic Pm-3m space group symmetry like most of the rare-earth hexaborides (REB6), resembling the crystal structure of CsCl. Rare-earth ion and octahedral B6 occupy Cs site and Cl site respectively, and the octahedral B6 cluster links to each other by strong covalent bonds providing high hardness characteristics.

YbB6 is traditionally synthesized through mechano-chemical processes, high temperature sintering methods, vacuum calcination, and combustion synthesis.

Molar mass：237.96 g/mol

Solubility in water：insoluble

Crystal structure：Cubic

Chemical Composition

|  | Major constituent |  | Impurity(≤) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Item | B | Yb | Fe | C | Mg | Si | Ca | Mn | Cu | Cr |
| Content(%) | 25.77 | 73.85 | 0.028 | 0.19 | 0.00029 | 0.0045 | 0.0079 | 0.0007 | 0.00030 | 0.0006 |

Granularity of materials -360 mesh

Application

Rare earth and alkaline earth hexaborides have potential uses in a variety of engineering applications because of their unique electrochemical and magnetic properties.

Ytterbium hexaboride (YbB6) has a unique conductive surface and has broad application prospects in engineering applications. Its unique properties also enhance the possibility of selective adsorption of small molecules to the YbB6 surface. Therefore, YbB6 is also a potential sensing material.

Ytterbium Boride Synonyms

Ytterbium hexaboride

Package:

Vacuum pumping and argon protection, 500g or 1000g / bottle