Molecular Formula: TbH2~3

Purity:99.9%

Specification:- 200 mesh / -100mesh/ - 5µm

CAS:13598-54-4

EINECS No.:237-071-4

# Terbium hydride(TbH2~3)-Powder

Characteristic

Terbium hydride is a compound of hydrogen and terbium. It is considered to be a part of the class of rare-earth metal hydrides. Metal hydrides are very attractive and important materials in the permanent magnets field. Terbium is a chemical element with the symbol Tb and atomic number 65. It is a silvery-white, rare earth metal that is malleable, ductile, and soft enough to be cut with a knife. Terbium is highly reactive. It should be stored in a container filled with inert gas or a vacuum container.

Appearance：Powder

Molecular Weight：161.95 g/mol

Density：N/A

Chemical Composition

| Rare Earth Impurity(≤) |  |  |  | Tb/RE |  | ≥99.9% |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Item | La/RE | Ce/RE | Pr/RE | Nd/RE | Sm/RE | Eu/RE | Gd/RE |
| Content(%) | 0.0002 | 0.0003 | 0.0002 | 0.0009 | 0.0001 | 0.0001 | 0.0011 |
| Item | Dy/RE | Ho/RE | Er/RE | Tm/RE | Yb/RE | Lu/RE | Y/RE |
| Content(%) | 0.0011 | 0.0001 | 0.0001 | 0.0001 | 0.0001 | 0.0001 | 0.0005 |
| Non-Rare Earth Impurity(≤) |  |  |  | RE |  | ≥99% |  |
| Item | Al | Fe | Ca | Si | Mg | C | O |
| Content(%) | 0.0270 | 0.0260 | 0.0280 | 0.0240 | 0.0210 | 0.0150 | 0.1400 |

Granularity of materials - 200 mesh

# Application

- Terbium hydride is the important additive for NdFeB permanent magnets to raise the Curie temperature and improve temperature coefficiency.

- Terbium hydride is used in the preparation of hydrogen storage alloys, catalysts, etc. in special fields such as aerospace, special metals and electronic lasers.

Package:

Vacuum pumping and argon protection, 500g or 1000g / bottle