- Molecular Formula: NdH2~3

- Purity:99.5%

- Specification:- 100 mesh / - 200 mesh

- CAS:13864-04-5

- EINECS No.:237-610-3

# Neodymium hydride (NdH2~3)-Powder

Characteristic

- Neodymium hydride is an inorganic compound composed of neodymium and hydrogen with a chemical formula NdH3. It is considered as the most common hydride of neodymium. In this compound, the neodymium atom is in the +3 oxidation state and the hydrogen atoms are -1. It is highly reactive Neodymium hydride is a blue crystal of the hexagonal system, with unit cell parameters a=0.385 nm, c=0.688 nm. It reacts with water to form neodymium hydroxide and hydrogen gas.

Appearance：Powder

Molecular Weight：147.27 g/mol

Density：N/A

Chemical Composition

| Rare Earth Impurity(≤) |  |  |  | Nd/RE |  | ≥99.5% |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Item | La/RE | Ce/RE | Pr/RE | Sm/RE | Y/RE |  |  |
| Content(%) | 0.012 | 0.020 | 0.020 | 0.010 | 0.001 |  |  |
| Non-Rare Earth Impurity(≤) |  |  |  | RE |  | ≥99% |  |
| Item | Fe | Si | Ca | Mg | Al | C | Mo |
| Content(%) | 0.241 | 0.010 | 0.010 | 0.010 | 0.010 | 0.039 | 0.033 |

Granularity of materials- 200 mesh

# Application

- A important use of neodymium hydride is as a component in the alloys used to make high-strength neodymium magnets-powerful permanent magnets.

- Adding neodymium to magnesium or aluminum alloy can improve the high temperature performance, air tightness and corrosion resistance of the alloy, and is widely used as an aerospace material.

Package:

Vacuum pumping and argon protection, 500g or 1000g / bottle